|  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Item** | **Product** | **Material** | **Hardness (HRC)** | **Diameter (mm)** | **Length (mm)** | **Head** | **Point** | **Surface Treatment** |
| Y-13A | washered steel nail | Steel | 54° ~ 57° | 3.7 | 25 ~ 75 | flat) | needle | Zinc Plating |
| Y-13B | washered steel nail | Steel | 54° ~ 57° | 3.7 | 25 ~ 75 | flat | needle | Zinc Plating |
| Y-13C | washered steel nail | Steel | 54° ~ 57° | 3.7 | 25 ~ 75 | flat | needle | Zinc Plating |
| Y-13D | washered steel nail | Steel | 54° ~ 57° | 2.5~3.7 | 25 ~ 75 | flat | needle | Zinc Plating |
| Y-13E | washered steel nail | Steel | 54° ~ 57° | 2.5~3.6 | 25 ~ 75 | flat | needle | Zinc Plating |